Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

GMAW(GAS METAL ARC WELDING)(MIG) #18 PROCEDURE: Select proper equipment for GMAW process. Cut one piece ¼” x 5” x 5” mild steel plate Set machine according to chart located inside panel Wire side is .035 Set Argon/CO² to 25 psi Re-adjust if necessary Use proper welding techniques for flat position. ONE SIDE ONLY – deposit a series of adjacent parallel beads to cover an area 4 x 4 inches. Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed Deposit a second series of parallel beads over the first layer at right angles to the first. Deposit a third series of parallel beads over the second layer at right angles to the second. Once completed, clean welds before presenting to instructor. DO NOT TURN IN HOT METAL GMAW ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 8 pts _______________ Evidence of slag inclusion 3 pts ________________ Overlapping techniques 10 pts ________________ Penetration 2 pts ________________ Comment: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

BEAD PAD – E6011 & E7018 #1 & 2 PROCEDURE: Select proper equipment for electric arc welding. Use one side E6011 the opposite side of the E7018 pad Set amperage setting 90-100 Set polarity lever to DC only Re-adjust if necessary Use proper welding techniques for flat position. ONE SIDE ONLY – deposit a series of adjacent parallel beads to cover an area 4 x 4 inches. Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed Chip and clean all slag thoroughly before depositing a second layer Deposit a second series of parallel beads over the first layer at right angles to the first. Deposit a third series of parallel beads over the second layer at right angles to the second. Once completed, clean welds before presenting to instructor. DO NOT TURN IN HOT METAL E6011 & E7018 Scorecard E6011 E7018 Follow direction: 2 pts _______¦________ Bead width 10 pts _______¦________ Uniformity of beads 10 pts _______¦________ Evidence of undercuts 5 pts _______¦________ Evidence of porosity 5 pts _______¦________ Evidence of slag inclusion 6 pts ________¦________ Overlapping techniques 10 pts _______¦_________ Penetration 2 pts _________________ Comments: Total 50 pts _______¦_________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

LAP WELD – E6011 ONLY FLAT ONLY #3 PROCEDURE: Select proper equipment for electric arc welding. Cut 2 - ¼” x 2” x 4” mild steel flat bar(use ¼ x 2” Flat bar) Select 1/8” E 6011 electrode Set amperage setting 90-100 and adjust accordingly Set polarity lever to AC only. Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) Tack weld both ends of plates. Use a single bead one side and overlapping beads to cover the lab joint on the opposite side. Keep the electrode at an angle of from 30 to 45 degrees with the lower plate Hold the arc slightly longer on the lower plate. Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 8 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

LAP WELD – E7018 ONLY FLAT ONLY #4 PROCEDURE: Select proper equipment for electric arc welding. Cut 2 - ¼” x 2”x 4” mild steel flat bar(use ¼ x 2” Flat bar) Select 1/8” E7018 electrodes Set amperage setting 90-100 and adjust accordingly. Set polarity lever to DC only Place the two pieces of metal so they overlap ¼ to ½ inch. (protect your finished work from spatter.) Tack weld both ends of plates. Use a single bead pass on one side and overlapping beads to cover the lab joint on opposite side. Keep the electrode at an angle of from 30 to 45 degrees with the lower plate Hold the arc slightly longer on the lower plate. Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 8 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

TEE FILET – E6011 ONLY FLAT ONLY #5 PROCEDURE: Select proper equipment for electric arc welding. Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar(use ¼ x 2” Flat bar) Select 1/8” E 6011 electrode Set amperage setting 90-100 and adjust accordingly. Set polarity lever to AC only. Set two pieces together at right angles forming a tee joint and tack weld both ends. Make one bead pass on one side and three overlapping bead passes to complete the fillet weld on opposite side. Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 4 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

TEE FILLET – E7018 ONLY FLAT ONLY #6 PROCEDURE: Select proper equipment for electric arc welding. Select 1/8” E7018 electrodes Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar(use ¼ x 2” Flat bar) Set amperage setting 90-100 and adjust accordingly. Set polarity lever to DC only Set two pieces together at right angles forming a tee joint and tack weld both ends. Make one bead pass on one side and three overlapping bead passes to complete the fillet weld on opposite side. Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 4 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

LAP WELD – E6011 ONLY VERTICAL ONLY #7 PROCEDURE: Select proper equipment for electric arc welding. Cut 2 pieces - ¼” x 2”x 4” mild steel flat bar Select 1/8” E 6011 electrode Set amperage setting 90-100 and adjust accordingly Set polarity lever to AC only. Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) Tack weld both ends of plates. Make a one bead pass on one side and overlapping bead passes to complete the fillet weld on opposite side. Keep the electrode at an travel angle of 30 to 45 degrees with the lower plate Hold the arc slightly longer on the lower plate. Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

LAP WELD – E7018 ONLY HORIZONTAL ONLY #8 PROCEDURE: Select proper equipment for electric arc welding. Cut 2 pieces -¼” x 2” x 4” mild steel flat bar Select 1/8” E7018 electrodes Set amperage setting 90-100 and adjust accordingly. Set polarity lever to DC only Place the two pieces of metal so they overlap 1 inch. (protect your finished work from spatter.) Tack weld both ends of plates. Make a one bead pass on one side and overlapping bead passes to complete the fillet weld on opposite side. Keep the electrode at an travel angle of 30 to 45 degrees with the lower plate Hold the arc slightly longer on the lower plate. Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL E7018 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

TEE FILET – E6011 ONLY VERTICAL ONLY #9 PROCEDURE: Select proper equipment for electric arc welding. Cut 2 pieces- ¼” x 2”x 4” mild steel flat bar. Select 1/8” E 6011 electrode Set amperage setting 90-100 and adjust accordingly. Set polarity lever to AC only. Set two pieces together at right angles forming a tee joint and tack weld both ends. Make 3 overlapping passes to complete the fillet weld on each side. Use proper techniques welding in vertical position only. DO NOT TURN IN HOT METAL E6011 ONLY Scorecard Follow direction: 2 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 6 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 10 pts ________________ Penetration 5 pts ________________ Comments: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

Y-ACETYLENE PUDDLE PAD #10 MATERIALS: 1 piece of 16 ga. 3”x4” plate steel #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: Cut plate steel according to specification. Plate steel must be off the tabletop. Place any type of scrap metal beneath the plate. For welding only, set acetylene & oxygen line pressure gages equal. Set approximately 4-5 psi on both line pressure gages. Use a # 0, or #1 tip size Re-adjust if necessary Use proper techniques welding in flat position only. Use a circular or half moon motion to obtain desired width of bead. Separate each bead approximately ½”. Make 5 consecutive beads with maximum penetration. Clean with wire brush and turn in. DO NOT TURN IN HOT METAL PUDDLE PAD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

OXY-ACETYLENE BEAD PAD/ROD #11 MATERIALS: 1 piece – 16 ga. 3”x4” plate steel 1/8” bare rod #1 or #2 welding tip PROCEDURE: Cut plate steel according to specification. Plate steel must be off the tabletop. Place any type of scrap metal beneath the plate. For welding only, set acetylene & oxygen line pressure gages equal. Set approximately 4-5 psi on both line pressure gages. Re-adjust if necessary Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL BEAD /WITH ROD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

OXY-ACETYLENE CORNER WELD #12 MATERIALS: 2 pieces of 16 ga.1-1/2”x4” plate steel #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: Cut plate steel according to specification. Set the material together tent-like on the welding table Tack the ends to prevent distortion. Weld with a semi-circular motion of the torch tip. Hold tip of inner luminous cone from 1/32 to 1/16 inch from work at 45degree angle. Set approximately 4-5 psi on both line pressure gages. Use a # 0, or #1 tip size Re-adjust if necessary Use proper oxy-acetylene welding techniques.. Clean with wire brush and turn in. DO NOT TURN IN HOT METAL CORNER WELD Scorecard Follow direction: 4 pts _______________ Bead width 8 pts _______________ Uniformity of bead 5 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 15 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

OXY-ACETYLENE BRAZE WELDING #13 MATERIALS: 2 pieces – 16ga. x 1-1/2”x4” plate steel Brazing rod with flux #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: Cut plate steel according to specification. Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. Make sure pieces fit tightly together. Preheat total area to 1600 degrees F. or cherry red color. Apply brazing flux with rod to area where brazing material is to adhere. Tin weld with thin coating of brazing filler rod. Build up brazing filler material to proper thickness. Clean excess flux from weld by buffing or chisel. DO NOT TURN IN HOT METAL BRAZING LAP WELD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

OXY-ACETYLENE BRAZE WELD PIPE FILLET WELD #14 MATERIALS: 1 piece of 16 ga x 2”x 2” plate steel 1 piece of 1-1/2” diameter x 1-1/2” conduit pipe #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: Cut plate steel according to specification. Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. Make sure pieces fit tightly together. Preheat total area to 1600 degrees F. or cherry red color. Apply brazing flux with rod to area where brazing material is to adhere. Tin weld with thin coating of brazing filler rod. Build up brazing filler material to proper thickness. Clean excess flux from weld by buffing or chisel. Pour water inside conduit pipe to test for water holding capabilities. DO NOT TURN IN HOT METAL PIPE FILLET WELD Scorecard Follow direction: 4 pts _______________ Bead width 5 pts _______________ Uniformity of beads 5 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 10 pts ________________ Water holding capabilities 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

OXY-ACETYLENE BRAZE WELD LAP JOINT #15 MATERIALS: 2 pieceS – 16 gax 2”x ” mild steel plate Brazing rod with flux #0 or #1 tip, neutral flame, equal oxygen and acetylene pressures. PROCEDURE: Cut plate steel according to specification. Mechanically clean flat base piece and edges of approximately ½ inch with a grinder. Make sure pieces fit tightly together. Preheat total area to 1600 degrees F. or cherry red color. Apply brazing flux with rod to area where brazing material is to adhere. Tin weld with thin coating of brazing filler rod. Build up brazing filler material to proper thickness. Clean excess flux from weld by buffing or chisel. DO NOT TURN IN HOT METAL BRAZING LAP WELD Scorecard Follow direction: 4 pts _______________ Bead width 10 pts _______________ Uniformity of beads 10 pts _______________ Bead appearance 10 pts _______________ Techniques used 5 pts ________________ Penetration 8 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

OXY-ACETYLENE CUTTING #16 MATERIALS: 1 piece – 1/4”x 5” steel bar PROCEDURE: Cut steel bar according to specification, illustrated below. Measure & mark layout Use a try square & soapstone to square end. Use proper procedures in setup & operating oxy-acetylene equipment. If necessary, use a tip cleaner to clean orifices. Align the orifices in a manner to permit preheat holes to lead and follow the cut. Use chart to determine acetylene & oxygen pressures for operation. Cut marked area. Have instructor check cut area before attempting to make other cuts. Cut according to specifications. DO NOT TURN IN HOT METAL 2” cuts 5” OXY-ACETYLENE CUTTING SKILL Scorecard Follow direction: 3 pts _________________ Measurements 10 pts __________________ Uniform cuts 10 pts __________________ Visible slag 5 pts _________________ Gouging 6 pts _________________ Proper angle of cut 8 pts ________________ Evidence of beveling 5 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

PLASMA CUTTING #17 MATERIALS: 1 piece – 3/16”x 5”x ”x 5” steel plate PROCEDURE: Cut steel bar according to specification, illustrated below. Measure & mark layout Use a try square & soapstone to square end. Use proper procedures in setup & operating plasma cutting equipment. Clean tip orifices. Use chart to determine air pressures for cutting operation. Cut marked area. Cut according to specifications. DO NOT TURN IN HOT METAL 1” circle 5” 1” 2” 2” 1” 2” Scorecard Follow direction: 3 pts _________________ Measurements 20 pts __________________ (According to Plan) Uniform cuts 15 pts __________________ Visible slag 10 pts _________________ Safety 2 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – GMAW WELDING

SCORECARD

BEAD PAD(OVERLAPPING) GMAW(GAS METAL ARC WELDING)(MIG) #18 PROCEDURE: Cut 2 – 3/16” x 2”x 6” plate steel Select proper voltage according to chart located inside machine. Set the wire speed according to chart located inside the machine May need to adjust wire according to sound and welding c. Re-adjust if necessary Use proper welding techniques for flat position. ONE SIDE ONLY – deposit a series of adjacent parallel beads to cover an area 4 x 4 inches. Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed Chip and clean all slag thoroughly before depositing a second layer Deposit a second series of parallel beads over the first layer at right angles to the first. Deposit a third series of parallel beads over the second layer at right angles to the second. Once completed, clean welds before presenting to instructor. DO NOT TURN IN HOT METAL GMAW ONLY Scorecard Follow direction: 3 pts _______________ Bead width 8 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 8 pts _______________ Evidence of porosity 4 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 8 pts ________________ Penetration 4 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – GMAW WELDING

SCORECARD

TEE FILLET GMAW(GAS METAL ARC WELDING)(MIG) #19 PROCEDURE: Cut 2 – 3/16” x 2”x 4” plate steel Select proper voltage according to chart located inside machine. Set the wire speed according to chart located inside the machine May need to adjust wire according to sound and welding c. Place the two pieces of metal so they overlap ¼ to ½ inch. (protect your finished work from spatter.) Tack weld both ends of plates. Use single to cover the lab joint. Hold the arc slightly longer on the lower plate. Use proper techniques welding in flat position only. DO NOT TURN IN HOT METAL GMAW ONLY Scorecard Follow direction: 3 pts _______________ Bead width 10 pts _______________ Uniformity of beads 6 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of porosity 5 pts _______________ Evidence of slag inclusion 6 pts ________________ Overlapping techniques 7 pts ________________ Penetration 5 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

Face/Root Stress Test #20 & #21 PROCEDURE: Select proper equipment for electric arc welding. Cut 2 - ¼” x 4”x 5” plate steel Select 1/8” E 6011 electrode Set amperage setting between 90-100, AC ONLY Use proper techniques for flat position welding. Space the metal parts approximately 1/8” apart. Tack weld both ends to prevent distortion Position the metal for welding and run a single stringer pass for penetration, tilting the electrode approximately 15 to 30 degrees from vertical in direction of travel. Upon completion of weld, chip slag and brush the weld clean. Make two overlapping cover pass for uniformity and quality of weld. Once completed, clean welds before presenting to instructor. Use available paint marker to mark your plate specimen. DO NOT TURN IN HOT METAL Discard discard Cut- Keep keep Cut-- Keep keep cut- Keep keep cut Discard discard 1/8” Use OA cutting torch or metal shear to cut 1 inch strips for testing. Discard strips as indicate above. Mark one strip with the letter “F” for face bend (side that has the weld bead) Mark the other two with the letter “R” for root bend (non-welded side) Use bench or hand grinder, to grind the welds smooth. Take strips to weld tester, place the side marked “F” face down on rollers and the plunger on center of weld joint. Same procedure is used for the root bend. E6011 ONLY Scorecard FACE ROOT Follow direction: 10 pts ___________ ___________ Preparation 10 pts ___________ ___________ Evidence of undercuts 5 pts ___________ ___________ Evidence of slag inclusion 5 pts ___________ ___________ Meet stress test 20 pts ___________ ___________ Total 50 pts ___________ ___________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

ELECTRIC ARC WELDING PIPE FILLET WELD #22 MATERIALS: 1 piece of ¼”x 3”x 3” plate steel 1 piece of 2” diameter x 2” black pipe E6011 & or E7018 electrodes PROCEDURE: Cut plate steel & pipe according to specification. Place pipe in center of base metal Use E6011 electrode for a stringer pass Use E7018 electrode for a cover pass Check for leaks by pouring water into pipe and let stand DO NOT TURN IN HOT METAL PIPE FILLET WELD Scorecard Follow direction: 4 pts ________________ Bead width 5 pts _________________ Uniformity of bead 5 pts _________________ Bead appearance 10 pts _________________ Techniques used 5 pts ________________ Penetration 7 pts ________________ Water holding capabilities 10 pts ________________ Safety 3 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1352 – WELDING

SCORECARD

Irregularities in Weldment #23 PROCEDURE: Select proper equipment for electric arc welding. Cut one piece 1-1/2 X 1-1/2 X 4” angle iron Set amperage setting accordingly Set polarity lever to AC only Re-adjust if necessary Use proper welding techniques for flat position. Each bead must be overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed Chip and clean all slag thoroughly before depositing a second layer to prevent slag inclusions. Deposit enough welds to fill the “V” portion of angle iron You may cool the specimen in water. Once cool, use power saw to cut in two pieces (2 inches in length) Tack weld two piece together to form a “W” DO NOT TURN IN HOT METAL 6011 and/or 7018 Scorecard Follow direction: 5 pts _______________ Bead width 5 pts _______________ Uniformity of beads 5 pts _______________ Evidence of undercuts 5 pts _______________ Evidence of slag inclusion 30 pts ________________ (1 point deduct for each Inclusions) Comment: Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept