Name: ____________________________________________

Date Completed: ___________________________________

### TOOL CONDITIONING

### SCORECARD

SHARPENING A TWIST DRILL- FREE HAND Materials needed: Dull twist drill Safety glasses Angle template or gauge Grinder with adjustable tool rest Container of water Procedure and Illustration Place the drill point against the grinding wheel at approximately a 59-degree angle. Use one hand near the bit point and wheel; raise the bit cutting point and, at the same time, lower the shank slightly with the other hand during the cutting process. This should form a clearance angle of about 12 degrees. Use a template to check the proper angle after every stroke. Determine the proper lip clearance by holding the drill bit in a horizontal position and level with the eye. The point or centerline formed by grinding both lips should be 45 degrees to the cutting edge. TWIST DRILL Scorecard Cutting lip angles 10 pts _______________ Dead Center angle 10 pts _______________ Heal angle 10 pts _______________ Signs of overheating 5 pts _______________ Smooth surface 5 pts ________________ Length of cuttings 5 pts ________________ Safety 5 pts ________________ Total 50 pts ________________

Texas A&M University-Kingsville – Ag Mechanics Dept

Name: ____________________________________________

Date Completed: ___________________________________

AGSC 1451 – WELDING

SCORECARD BEAD PAD – E6013ONLY PROCEDURE: Select proper equipment for electric arc welding. Select ¼” x 5” x 5” plate steel Set amperage setting 90-100 Set polarity lever to AC only Re-adjust if necessary Use proper welding techniques for flat position. ONE SIDE ONLY – deposit a series of adjacent parallel beads covering an area 4 x 4 inches Each bead must be run in contact, overlapping ¼ to ½ way with the adjoining bead so that a continuous layer of metal is formed Chip and clean all slag thoroughly before depositing a second layer Deposit a second series of parallel beads over the first layer at right angles to the first. Deposit a third series of parallel beads over the second layer at right angles to the second. Once completed, clean welds before presenting to instructor. DO NOT TURN IN HOT METAL E6013 ONLY Scorecard Follow direction: 3 pts _____________ Bead width 10 pts ______________ Uniformity of beads 6 pts _____________ Evidence of undercuts 5 pts _____________ Evidence of porosity 5 pts _____________ Evidence of slag inclusion 6 pts ______________ Overlapping techniques 7 pts ______________ Penetration 5 pts ______________ Safety 3 pts ______________ Total 50 pts ______________

Texas A&M University-Kingsville – Ag Mechanics Dept